A study of CO adsorption on CaY zeolite by DFT calculation

Shergin Yaroslav

st054872@student.spbu.ru

Scientific supervisor: Prof. Tsyganenko A.A. Faculty of Physics, Saint-Petersburg State University

FTIR spectra of CO adsorbed on Ni-containing USY zeolites show the formation of mono-, di-, and tricarbonyls with Ni+ cations, characterized by one, two or three well resolved bands which shift in a certain way on 13C substitution [1]. In earlier studies of linkage isomerism of CO adsorbed on CaY zeolite [2, 3] adsorption of two molecules on the same cation was manifested in a shift of CO stretching band with coverage, which does not split in two maxima as expected for the dicarbonyl. Band assignment in the spectra of adsorbed 12CO-13CO mixtures faced some difficulties. For better understanding the experimental results we have carried out a DFT calculation of one or two CO molecules interacting with Ca cation in a cluster modelling a fragment of zeolite framework. The calculated frequency values compared with those observed experimentally in [2,3] are presented in Table 1. The calculated values of harmonic frequencies were multiplied by scaling coefficients different for C- or O- bonded molecules.

Table 1. Experimental and calculated frequencies for Ca++ carbonyls in Y zeolite

|  | 12CO | O12C | 13CO | O13C |
| --- | --- | --- | --- | --- |
| exp. cm-1 | 2197 | 2094 | 2150-2149 | 2048 |
| calc. cm-1 | 2198,5 | 2094,0 | 2149,2 | 2047,2 |
|  | 12CO12CO | 12CO13CO | 13CO13CO | 12CO12OC |
| exp. cm-1 | 2191 | 2191 | 2142-2140 | 2211?; 2099 |
| calc. cm-1 | 2197,5; 2188,9 |  |  | 2189,9; 2101,3 |

Analysis of the obtained results demonstrates a good agreement between the observed and calculated values and shows that due to weaker interaction between the two molecules in dicarbonyls the splitting is small and the second band of CO vibration coincides with that of monocarboonyl. Assignment of a shoulder at 2211 cm-1 to C-bonded molecule in dicarbonyl structure, proposed in [3], does not agree with the calculation.

Acknowledgement

The work was supported by RFBR and CITMA, grant No. 18-53-34004. The author thanks the Computing Center of St.PbU for the computing facilities.

References

- R.Belykh, F.Mauge, A.Tsyganenko. Applied Catalysis A. 583 (2019) 117140.

- A.Tsyganenko, P.Storozhev, C.Otero Areán. Kinet. Catalysis, 45 (2004) 530.

- Tsyganenko A.A. In: Aspects of the Surface Chemistry of Oxidic Systems. Proc. Symp. in Honour of E.Escalona Platero. Torino. 1999, p.51.